## Slide 1
DEVELOPMENT OF ELECTROCONDUCTIVE MATERIALS BASED ON METALLIZED POLYIMIDES AS ELEMENTS OF FLEXIBLE SOLAR CELLS
Rinat Iskakov
KBTU
Korean seminar October 23, 2015 год

## Slide 2
riskakov@mail.ru r.iskakov@kbtu.kz http://www.chemistry.kz
Korean seminar October 23, 2015 год
BAKDAULET SEIFULLIN,
ARAILYM IBRAIMBEK,
ERNUR TOLEP,
KAMSHAT UMBETOVA,
RINAT ISKAKOV
VICTORIA KHEGAY

## Slide 3
Korean seminar October 23, 2015 год

## Slide 4
Conductive layer: PEDOT: PSS –
Acceleration & transportation of charge
Photoactive layer: P3HT/PCBM – semiconductive transmitter
Cathode: Metal for electron accumulation
Korean seminar October 23, 2015 год

## Slide 5
Transmission coefficient- more 85%
Resistivity of surface layer- less 100 (Ohm per sq.sm)
Quality standard is transparency degree
1.5 см
Volume EG %
Annealing temperature
Film thickness
1.5 см
Korean seminar October 23, 2015 год

## Slide 6
1) Optimization of additive amount (EG)
Conditions: 5000 rpm, T = 150 0С
Result: solution of 6% EG
Korean seminar October 23, 2015 год

## Slide 7
2) Optimization of annealing temperature
Condition: 5000 rpm, р-р 6% EG
  Results: 140 0С
Korean seminar October 23, 2015 год

## Slide 8
3) Thickness optimization
Conditions: solution of 6% EG, T = 140 0С
Korean seminar October 23, 2015 год

## Slide 9
Result: 800 rpm (126 нм) .
4) Surface resistivity vs transparency
Korean seminar October 23, 2015 год

## Slide 10
Amount of ethyleneglycol(EG) - 6%.
Annealing temperature 140 ℃
Film thickness 125 nm
Optimal conditions
Korean seminar October 23, 2015 год

## Slide 11
Optimization of active layer thickness
Optimization of drying temperature after annealing
Korean seminar October 23, 2015 год

## Slide 12
1) Optimization of active layer thickness
Result: 3500 rpm (90 nm) .
Korean seminar October 23, 2015 год

## Slide 13
2) Temperature optimization after annealing
Results: 150 ℃ .
Korean seminar October 23, 2015 год

## Slide 14
Thickness of the active layer at 3500 rpm (90 nm)
Temperature after annealing- 150 ℃
PCE мax: 3.3 % (transmittance efficiency)
Korean seminar October 23, 2015 год

## Slide 15
Alkali hydrolisys
Ion chelation
Metal reduction
Annealing
50-100 nm
PI film
Metallized PI film
Korean seminar October 23, 2015 год

## Slide 16
1. Alkali hydrolisys
2. Ion chelation
3. Metal reduction
Korean seminar October 23, 2015 год

## Slide 17
Ag
Ag
ПИ
PI films concentrate Ag crystals at the surfaces
Korean seminar October 23, 2015 год

## Slide 18
METALL
POLYIMIDE
Ag
Metal nanostructures with “dead adhesion”
Korean seminar October 23, 2015 год

## Slide 19
c
Korean seminar October 23, 2015 год

## Slide 20
METALL
POLYIMIDE
Korean seminar October 23, 2015 год

## Slide 21
From left: the initial solution; during; and after synthesis
TEM of silver nanoparticles
Diffraction
AgAc
AgNO3
Korean seminar October 23, 2015 год

## Slide 22
TEM of silver nanoparticles in DMFA
а
б
в
Korean seminar October 23, 2015 год

## Slide 23
Dependence of plasmon max of silver nanoparticles on synthesis duration
Salt AgNO3 (●) and AgAc (○) in DMFA (а) and ethanol (б)
Korean seminar October 23, 2015 год

## Slide 24
TEM of Co (а, б) and Ni (в) nanoparticles and their size distribution
а
в
б
DMFA
DMFA
DMSO
Korean seminar October 23, 2015 год

## Slide 25
riskakov@mail.ru r.iskakov@kbtu.kz http://www.chemistry.kz
Korean seminar October 23, 2015 год
감사합니다