## Slide 1: MICROSPHERES – APPLICATION PROSPECTS AS SORBENTS IN ENERGY SAVING TECHNOLOGIES

## Slide 2: what is a cenosphere?
The cenosphere is a lightweight, inert, hollow sphere made largely of silica and alumina and filled with air or inert gas., typically produced as a byproduct of coal combustion at thermal power plants. The color of cenospheres varies from gray to almost white and their density is about 0.4–0.8 g/cm3

## Slide 3
Cenosphere
oil production and chemical industry
materials for oil wells
drilling mud
explosives
catalysts
defoamers
Building Industry
lime mixtures
mastic, plaster
super lightweight concretes
sound proof materials
insulation and roofing surfaces
dry mix
abrasive highly porous materials
refractory Industry
lightweight refractory material
insulating materials
nylon, plastic, and other materials of different densities
polymer industry
repair filler and primer
vehicle structure
tires, bumpers and panels
sound proof
materials
composites
Area of application
Cenospheres are being used in different industrial applications, mainly due to their low density, high strength, and good thermal properties. However, it is important and mandatory to study and characterize these ash particles for a better and effective usage.

## Slide 4: Extraction of microspheres
Russia, Kazakhstan
China
The apparent density of cenospheres is less than that of water and they float on the ash slurry. This property of the microspheres is used to collect them from the surface of technological water solutions of power station with a small nets or using of flotation methods

## Slide 5: Scheme of column flotation
The column flotation based on different principle distribution of water between the foam and the chamber product showed the possibility of obtaining a more rich concentrates and diminish several stages of purification processes of mineral materials

## Slide 6: Separation of microspheres by using of column flotation cell
a)
b)

## Slide 7: The results of analyses
Спектр | В стат. | O | F | Mg | Al | Si | S | K | Ca | Ti | P | Fe | Na | Cl | ИТОГО
Спектр | Да | 48,96 | 0,66 | 0,26 | 18,31 | 24,45 | 0,09 | 0,42 | 2,18 | 1,01 | 0,65 | 2,53 | 0,37 | 0,11 | 100,00

## Slide 8
Where and how we can use them?

## Slide 9: Diagram in-situ leaching of uranium
Sometimes is taking place a spills of uranium solutions to the land

## Slide 10: Uranium mines

## Slide 11
The influence of radiation on a living organism
The Consequences of the Chernobyl Nuclear Power Plant and Semipalatinsk nuclear polygon

## Slide 12
Ceolit
Geotechnological barrier around Chernobyl nuclear power station
They filled out the trench of ceolites to prevent ingress of radioactive water into the river

## Slide 13: An accommodation option of filters in sewage ponds

## Slide 14: Experimental and technological testing
Sorption of uranium and rhenium

## Slide 15
№ | № sample | Time, hour | Content of U in solution, мg/dм3 | Content of Fe solution, мg/dм3
0 | 0 |  | 53,63 | 657,4
1 | 3.1 | 2 | 42,66 | 387,4
 | 3.2 | 4 | 42,13 | 408,5
 | 3.3 | 6 | 40,30 | 404,9
2 | 4.1 | 2 | 39,19 | 510,6
 | 4.2 | 4 | 41,68 | 476,6
 | 4.3 | 6 | 41,22 | 449,4
3 | 7.1 | 2 | 35,61 | 190,2
 | 7.2 | 4 | 23,82 | 316,9
 | 7.3 | 6 | 31,37 | 244,9
Content of uranium and iron infiltrate
 | Обьем на выходе | Металл, г/л | Степень извлечения по металлу, % | Кислотность, г/л
Темирт. Исх. | 5 | 37,18 | 61,27 | 4,9
Темирт. Кис. | 4 | 30,92 | 74,23 | 3,43
Темирт. Щел. | 4 | 14,33 | 88,06 | 0
Экиб. Исх. | 5 | 44,2 | 53,96 | 3,675
Экиб. Кисл. | 4 | 51,6 | 57,00 | 4,9
Экиб. Щел. | 4 | 39,89 | 66,76 | 0
Исх. Алматы | 6 | 80 | 0,00 | 3,92
Notes: № | № sample | Time, hour | Content of U in solution, мg/dм3 | Content of Fe solution, мg/dм3
0 | 0 |  | 53,63 | 657,4
1 | 3.1 | 2 | 42,66 | 387,4
 | 3.2 | 4 | 42,13 | 408,5
 | 3.3 | 6 | 40,30 | 404,9
2 | 4.1 | 2 | 39,19 | 510,6
 | 4.2 | 4 | 41,68 | 476,6
 | 4.3 | 6 | 41,22 | 449,4
3 | 7.1 | 2 | 35,61 | 190,2
 | 7.2 | 4 | 23,82 | 316,9
 | 7.3 | 6 | 31,37 | 244,9

## Slide 16
Leksin M.
Oserov T.
Kononov A.
Members of our team
Tyumenceva O.

## Slide 17
Almaty

## Slide 19
Thank you for attention!