## Slide 1
DEVELOPMENT OF Fe/N/C CATALYST FOR APPLICATION IN PROTON EXCHANGE MEMBRANE FUEL CELLS
Al-Farabi Kazakh National University
Faculty of Chemistry and Chemical Technology
Scientific and practical seminar
«Green energy and energy saving technologies in Kazakhstan»
Almaty, October 23, 2015
Rashid Nadirov

## Slide 2: Operating principle of the PEMFC
Invented in early 1960’s at General electric
First used by NASA to provide power for gemini space project
Operate at a temperature of around 80°C
Each cell produces around 0.7 volts
To generate high voltage, a number of individual cells are combined in series

## Slide 3: Advantages
Operate at low temperatures which allows them to start up rapidly from cold
High power density which makes them really compact and lightweight
PEMFC work at high efficiencies, producing around 40-50 percent of the maximum voltage, and can vary their output quickly to meet shifts in power demand
Needs pure hydrogen to operate as they are very susceptible to poisoning by carbon monoxide and other impurities
High price and scarcity of precious metals for catalysts
Pt/C, 0.05-0.4 mg/ sm2
!
Disadvantages

## Slide 4: Catalyzed Reactions
Anode :
H2 = 2e- + 2H+
Cathode :
4H+ + 4e- + O2 = 2H2O
(oxygen reduction reaction, ORR)
Limitating stage

## Slide 5: Fe/N/C –one of the major in research on PEMFC catalysts
Chen, Z., Higgins, D., Yu, A., Zhang, L., & Zhang, J. A review on non-precious metal electrocatalysts for PEM fuel cells //Energy & Environmental Science. – 2011. – Т. 4. – №. 9. – С. 3167-3192.
Jaouen, F., Proietti, E., Lefèvre, M., Chenitz, R., Dodelet, J. P., Wu, G., Zelenay, P. Recent advances in non-precious metal catalysis for oxygen-reduction reaction in polymer electrolyte fuel cells //Energy & Environmental Science. – 2011. – Т. 4. – №. 1. – С. 114-130.
Wu, G., More, K. L., Johnston, C. M., Zelenay, P. High-performance electrocatalysts for oxygen reduction derived from polyaniline, iron, and cobalt //Science. – 2011. – Т. 332. – №. 6028. – С. 443-447.
Othman R., Dicks A. L., Zhu Z. Non precious metal catalysts for the PEM fuel cell cathode //International journal of hydrogen energy. – 2012. – Т. 37. – №. 1. – С. 357-372.
Dombrovskis, J. K., Jeong, H. Y., Fossum, K., Terasaki, O., & Palmqvist, A. E. Transition metal ion-chelating ordered mesoporous carbons as noble metal-free fuel cell catalysts //Chemistry of Materials. – 2013. – Т. 25. – №. 6. – С. 856-861
Wu G., Zelenay P. Nanostructured nonprecious metal catalysts for oxygen reduction reaction //Accounts of chemical research. – 2013. – Т. 46. – №. 8. – С. 1878-1889
Shin, D., Jeong, B., Mun, B. S., Jeon, H., Shin, H. J., Baik, J., & Lee, J. On the Origin of Electrocatalytic Oxygen Reduction Reaction on Electrospun Nitrogen–Carbon Species //The Journal of Physical Chemistry C. – 2013. – Т. 117. – №. 22. – С. 11619-11624
Wang, Q., Zhou, Z. Y., Lai, Y. J., You, Y., Liu, J. G., Wu, X. L., Sun, S. G. Phenylenediamine-Based FeNx/C Catalyst with High Activity for Oxygen Reduction in Acid Medium and Its Active-Site Probing //Journal of the American Chemical Society. – 2014. – Т. 136. – №. 31. – С. 10882-10885.

## Slide 6
Wang, Q., Zhou, Z. Y., Lai, Y. J., You, Y., Liu, J. G., Wu, X. L., Sun, S. G. Phenylenediamine-Based FeNx/C Catalyst with High Activity for Oxygen Reduction in Acid Medium and Its Active-Site Probing //Journal of the American Chemical Society. – 2014. – Т. 136. – №. 31. – С. 10882-10885

## Slide 7: The main idea:
synthesis of the catalyst in accordance with the known technique;
electrochemical treatment of the sample synthesized;
comparison of the samples activity toward ORR before and after treatment.
Wang, Q., Zhou, Z. Y., Lai, Y. J., You, Y., Liu, J. G., Wu, X. L., Sun, S. G. Phenylenediamine-Based FeNx/C Catalyst with High Activity for Oxygen Reduction in Acid Medium and Its Active-Site Probing //Journal of the American Chemical Society. – 2014. – Т. 136. – №. 31. – С. 10882-10885

## Slide 8
Chart: 2θ
Chart: 2θ
2 stages cathodic treatment:
0,5 М NaCl + 0,5 M HCl, 30 min, Е=-0,8 В
0,025 М Na2S + 0,005 M NaCl , 0,7 mА/sм2 , 40 min, 80±5 0С.
XRD – patterns of samples before (a) and after (b) cathodic treatment
(a)
(b)
- Fe3S4
- Fe3S4

## Slide 9: The main results obtained
Chart: E, V
| 0.2 | 0.22 | 0.25 | 0.35000000000000031 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.60000000000000064 | 0.65000000000000135 | 0.70000000000000062 | 0.75000000000000122 | 0.8 | 0.85000000000000064 | 0.9 | 0.95000000000000062 | 1
электрохимически обработанный образец | -4 | -4 | -4 | -4 | -4 | -4 | -4 | -3.95 | -3.95 | -3.8 | -3.7 | -3.5 | -3 | -2 | -0.7 | -0.3 | -0.05
необработанный образец | -4 | -4 | -4 | -4 | -3.95 | -3.95 | -3.95 | -3.95 | -3.95 | -3.7 | -3.45 | -3.1 | -2.4 | -1.4 | -0.3 | -0.1 | -0.05
9.8 A/g at 0.8 V
12.2 A/g at 0.8 V
Activity:
ORR Polarazition Curves in Air Saturated in 0.1 M Н2SO4

## Slide 10
In Cooperation with Prof. Melika Hinaje,

## Slide 11
Thank you for your attention!